1/1

May 21, 2003

# Black Polyester Film Tape
9381

## Product description

Black polyester tape 9381 is pressure sensitive adhesive tape consisted of black polyester film and acrylic pressure sensitive adhesive, which is designed for light sheilding applications.

## Product construction

|  | Black polyester film |
| --- | --- |
|  | Acrylic adhesive |

## Properties

| Item | Unit | 9381 |  |
| --- | --- | --- | --- |
| Total thickness | mm | 0.07 |  |
| Poyester film thickness | mm | 0.038 |  |
| Tensile strength | N/cm | 55 |  |
| Elongation at break | % | 70 |  |
| Adhesion | N/cm | 3.3 |  |
| Visible radiation transmittance | % | 1200nm | 2.20 |
|  |  | 1100nm | 1.65 |
|  |  | 1000nm | 1.18 |
|  |  | 900nm | 0.78 |
|  |  | 800nm | 0.48 |
|  |  | 700nm | 0.26 |
|  |  | 600nm | 0.11 |
|  |  | 500nm | 0.03 |
|  |  | 400nm | 0.00 |
|  |  | 300nm | 0.02 |
|  |  | 200nm | 2.04 |

Test method for adhesion

Sample width:25mm, Substrate: Stainless Steel (SS304), Pressure: 2kg rubber roller once for each direction,

Dwell temp: room temperature (23℃) for 20min., Peel speed: 300mm/min.

*** End of document ***